#276 SYNTHETIC FOOD GRADE GEAR LUBE H-1

Synthetic Food Grade Gear Lube H-1 is a synthetic blend, anti-wear, extreme pressure food grade oil that is specially formulated for use in the lubrication of food, feed and pharmaceutical processing and packaging equipment, especially those pieces of equipment that are subjected to high loads and high moisture conditions.

Synthetic Food Grade Gear Lube H-1 meets the requirements for a USDA H-1 quality lubricant and the requirements of the United States Code of Federal Regulations 21CFR 178.3570, 178.3620(b), and 573.680 of the United States Food and Drug Administration’s Regulations.

Synthetic Food Grade Gear Lube H-1 can be used in the lubrication of all types of enclosed gear, chain guide, chain and conveyor applications where there is a chance of incidental contact with food, foodstuffs, drinking water, potable water or ground water may occur. Typically, these applications can be found in the following industries:

| Meat and Poultry Processing Plants | Egg Processing Plants |
| --- | --- |
| Fish and Seafood Processing Plants | Breweries and Wineries |
| Soft Drink and Bottling Plants | Vegetable and Fruit Processors |
| Cheese and Cheese Product Producers | Bakeries |
| Snack Food Manufacturers | Pasta Manufacturers |
| Pet Food and Animal Feed Producers | Oil Mills and Seed Cake Processors |
| Pharmaceutical and Drug Manufacturers | Cosmetic Manufacturers |
| Food and Beverage Container Manufacturers | Paper and Paperboard Manufactures |
| Water Well Drillers | Drinking and Potable Water Treatment Plants |

Continued on Next Page

TD-276 (Rev. 5/2011)

TD-276

Page 2

Synthetic Food Grade Gear Lube H-1 is blended from a combination of highest quality, highly refined, severely hydro-finished and purified non-toxic technical white polyalphaolefin (PAO) synthetic base fluids and technical white and U.S.P. grade paraffinic white oils available. These technical white PAO synthetic base fluids and technical white and U.S.P. grade paraffinic white oils provide Synthetic Food Grade Gear Lube H-1 with the following advantages:

- Excellent lubricity and film strength

- Superior oxidative stability

- Excellent resistance to thermal degradation

- A high viscosity index

- Excellent hydrolytic stability

- Excellent resistance to acidic compounds

- Very good low temperature properties

- A reduction in operating temperatures

- Compatibility with all types of seals and coatings

- Extended drain intervals

Blended into the technical white PAO synthetic base fluids and technical white and U.S.P. grade paraffinic white oils is a highly specialized non-toxic food grade approved additive package which provides the Synthetic Food Grade Gear Lube H-1 with the following outstanding performance features:

- Exceptional anti-wear and load carrying capabilities

- Excellent rust and corrosion inhibiting properties

- Enhanced oxidation stability

- Excellent anti-foam and air release properties

- Enhanced oxidation stability.

Further blended into Synthetic Food Grade Gear Lube H-1 is a unique blend of USDA and FDA acceptable preservatives. These food grade preservatives provide the product with an effective way to control, inhibit and retard the growth of bacteria, yeast and molds that may come into contact with Synthetic Food Grade Gear Lube H-1 during use. These preservatives are not an antiseptic or sterilizing agent but Synthetic Food Grade Gear Lube H-1 does effectively prevent bacterial growth and control microbiological proliferation if the lubricant becomes contaminated during use.

Continued on Next Page

TD-276

Page 3

| ISO Grade | 100 | 150 |  | 220 | 320 |  | 460 | 680 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| SAE Grade |  |  | 90 |  |  | 140 |  |  |
| AGMA Grade | 3EP | 4EP | ---- | 5EP | 6Ep | ---- | 7EP | 8EP |
| Specific Gravity @ 60(F/15.5(C | 0.8719 | 0.8783 | 0.84 | 0.8443 | 0.8789 | 0.86 | 0.8583 | 0.8843 |
| Viscosity @ 40(C cSt (ASTM D-445) | 90.00-100 | 144-165 | 190-255 | 200-250 | 320-345 | 300-449 | 420-470 | 619-635 |
| Viscosity @ 100(C cSt (ASTM D-445) | 10.50-13.50 | 15.00-21.50 | 19.00-23.00 | 16.50-23.50 | 29.00-35.00 | 35.00-42.00 | 35.00-40.00 | 50.00-60.00 |
| Viscosity Index (ASTM D-2270) | 118 | 130 | 113 | 120 | 134 | 154 | 128 | 149 |
| Flash Point (F/(C (ASTM D-92) | 428(/220( | 442(/228( | 440(/227( | 440(/227( | 450(/232( | 455(/235( | 455(/235( | 460(/238( |
| Fire Point (F/(C (ASTM D-92) | 440(/227( | 470(/243( | 470(/243( | 470(/243( | 470(/243( | 480(/249( | 480(/249( | 485(/252( |
| Pour Point (F/(C (ASTM D-92) | -15(/-26( | -10(/-23( | -10(/-23( | -10(/-23( | 0(/-18( | 0(/-18( | 0(/-18( | 10(/-12( |
| Copper Strip Corrosion Test (ASTM D-130) | 1a | 1a | 1a | 1a | 1a | 1a | 1a | 1a |
| Rust Test (ASTM D-665) |  |  |  |  |  |  |  |  |
| Procedure A (Distilled Water) | Pass | Pass | Pass | Pass | Pass | Pass | Pass | Pass |
| Procedure B (Salt Water) | Pass | Pass | Pass | Pass | Pass | Pass | Pass | Pass |
| Demulsibility Test (ASTM D-1401) |  |  |  |  |  |  |  |  |
| Oil-Water-Emulsion @ 20 minutes | 40-40-0 | 40-40-0 | 40-40-0 | 40-40-0 | 40-40-0 | 40-40-0 | 40-40-0 | 40-40-0 |
| Oxidation Stability Test (ASTM D-943) |  |  |  |  |  |  |  |  |
| Hours to TAN of 2 | 4000 | 4000 | 4000 | 4000 | 4000 | 4000 | 4000 | 4000 |
| Falex Continuous Load (ASTM D-3233) |  |  |  |  |  |  |  |  |
| Procedure A |  |  |  |  |  |  |  |  |
| Failure Load, lbs. | 1250 | 1250 | 1250 | 1360 | 1360 | 1500 | 1500 | 1500 |
| Four Ball Wear Test (ASTM D-4172) |  |  |  |  |  |  |  |  |
| (1hr/40kg/130(F(54(C)) |  |  |  |  |  |  |  |  |
| Wear Scar Diameter, mm | 0.45 | 0.45 | 0.45 | 0.45 | 0.4 | 0.35 | 0.35 | 0.3 |
| Timken EP Test (ASTM D-2782) |  |  |  |  |  |  |  |  |
| OK Load. lbs | 30 | 35 | 40 | 40 | 40 | 40 | 40 | 40 |
| Total Acid Number (ASTM D-664) | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 | 0.03 |
| % Evaporation Loss (ASTM D-2887) |  |  |  |  |  |  |  |  |
| @ 700(F/372(C | 7.0 | 5.5 | 3.8 | 3.8 | 3.8 | 4 | 4.0 | 4.1 |
| % Evaporation Loss (ASTM D-972) |  |  |  |  |  |  |  |  |
| 22 hours @ 225(F/107(C | 2 | 1.5 | 1.5 | 1.5 | 1.5 | 1 | 1 | 1 |
| Foam Test (ASTM D-892) |  |  |  |  |  |  |  |  |
| Sequence I | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 |
| Sequence II | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 |
| Sequence III | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 | 0/0 |
| FZG A/8.3/90 (ASTM D-5182) |  |  |  |  |  |  |  |  |
| Load Failure Stage | 11th | 11th | 12th | 12th | 12th | 12th | 12th | 12th |